Support Information

Content

Figure S1 the Ultraviolet spectra of PFIO…………………………………….………2

Figure S2 1H-NMR(400MHz, CDCl3) spectra of PFIO………………………..……..3

Figure S3 Crystal packing of PFIO…………………………………………………....4

Table S1 Element analysis result of PFIO……………………………….…………….4

Table S2 Crystal and experimental data of PFIO……………….………..……………5

Figure S1 the Ultraviolet spectra of PFIO

Figure S2 1H-NMR(400MHz, CDCl3) spectra of PFIO

Figure S3 crystal packing of PFIO

Table S1 Element analysis result of PFIO

|  | N% | C% | H% | O% |
| --- | --- | --- | --- | --- |
| Test 1 | 4.34 | 70.99 | 4.357 |  |
| Test 2 | 4.40 | 70.94 | 4.394 |  |
| Mean of Tests | 4.37 | 70.97 | 4.376 |  |
| Calculated value | 4.36 | 71.02 | 4.71 | 19.92 |

Table S2 Crystal and experimental data of PFIO

| Empirical formula | C19H15NO4 |
| --- | --- |
| Formula weight | 321.32 |
| Temperature/K | 293.15 |
| Crystal system | orthorhombic |
| Space group | Pbca |
| a/Å | 8.8615(7) |
| b/Å | 14.6666(10) |
| c/Å | 24.4247(19) |
| α/° | 90 |
| β/° | 90 |
| γ/° | 90 |
| Volume/Å3 | 3174.4(4) |
| Z | 8 |
| ρcalcg/cm3 | 1.345 |
| m/mm-1 | 0.095 |
| F(000) | 1344.0 |
| Crystal size/mm3 | 0.3 × 0.2 × 0.2 |
| Radiation | MoKα (λ = 0.71073) |
| 2θ range for data collection/° | 5.8 to 52.742 |
| Index ranges | -10 ≤ h ≤ 11, -18 ≤ k ≤ 18, -30 ≤ l ≤ 28 |
| Reflections collected | 14135 |
| Independent reflections | 3167 [Rint = 0.0206, Rsigma = 0.0201] |
| Data/restraints/parameters | 3167/0/217 |
| Goodness-of-fit on F2 | 1.029 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0492, wR2 = 0.1200 |
| Final R indexes [all data] | R1 = 0.0656, wR2 = 0.1309 |
| Largest diff. peak/hole / e Å-3 | 0.41/-0.18 |